## Slide 1
Prof.Manoj Salunke
(M.E.Production)
(Asst.Professor in Mechanical Engg.Dept.)
(*KCECOEM JALGAON*)

## Slide 2: 2
Stress and Strain – Axial Loading

## Slide 3: Contents
Stress & Strain: Axial Loading
Normal Strain
Stress-Strain Test
Stress-Strain Diagram: Ductile Materials
Stress-Strain Diagram: Brittle Materials
Hooke’s Law: Modulus of Elasticity
Elastic vs. Plastic Behavior
Fatigue
Deformations Under Axial Loading
Example 2.01
Sample Problem 2.1
Static Indeterminacy
Example 2.04
Thermal Stresses
Poisson’s Ratio
Generalized Hooke’s Law
Dilatation: Bulk Modulus
Shearing Strain
Example 2.10
Relation Among E, n, and G
Sample Problem 2.5
Composite Materials
Saint-Venant’s Principle
Stress Concentration: Hole
Stress Concentration: Fillet
Example 2.12
Elastoplastic Materials
Plastic Deformations
Residual Stresses
Example 2.14, 2.15, 2.16

## Slide 4: Stress & Strain: Axial Loading
Suitability of a structure or machine may depend on the deformations in the structure as well as the stresses induced under loading. Statics analyses alone are not sufficient.
Considering structures as deformable allows determination of member forces and reactions which are statically indeterminate.
Determination of the stress distribution within a member also requires consideration of deformations in the member.
Chapter 2 is concerned with deformation of a structural member under axial loading. Later chapters will deal with torsional and pure bending loads.

## Slide 5: Normal Strain

## Slide 6: Stress-Strain Test

## Slide 7: Stress-Strain Diagram: Ductile Materials

## Slide 8: Stress-Strain Diagram: Brittle Materials

## Slide 9: Hooke’s Law: Modulus of Elasticity
Below the yield stress
Strength is affected by alloying, heat treating, and manufacturing process but stiffness (Modulus of Elasticity) is not.

## Slide 10: Elastic vs. Plastic Behavior
If the strain disappears when the stress is removed, the material is said to behave elastically.
When the strain does not return to zero after the stress is removed, the material is said to behave plastically.
The largest stress for which this occurs is called the elastic limit.

## Slide 11: Fatigue
Fatigue properties are shown on S-N diagrams.
When the stress is reduced below the endurance limit, fatigue failures do not occur for any number of cycles.
A member may fail due to fatigue at stress levels significantly below the ultimate strength if subjected to many loading cycles.

## Slide 13: Example 2.01
Determine the deformation of the steel rod shown under the given loads.
SOLUTION:
Divide the rod into components at the load application points.
Apply a free-body analysis on each component to determine the internal force
Evaluate the total of the component deflections.

## Slide 14
SOLUTION:
Divide the rod into three components:
Apply free-body analysis to each component to determine internal forces,
Evaluate total deflection,

## Slide 15: Sample Problem 2.1
The rigid bar BDE is supported by two links AB and CD.
Link AB is made of aluminum (E = 70 GPa) and has a cross-sectional area of 500 mm2. Link CD is made of steel (E = 200 GPa) and has a cross-sectional area of (600 mm2).
For the 30-kN force shown, determine the deflection a) of B, b) of D, and c) of E.
SOLUTION:
Apply a free-body analysis to the bar BDE to find the forces exerted by links AB and DC.
Evaluate the deformation of links AB and DC or the displacements of B and D.
Work out the geometry to find the deflection at E given the deflections at B and D.

## Slide 16
Displacement of B:
Displacement of D:
Sample Problem 2.1
Free body: Bar BDE
SOLUTION:

## Slide 17
Displacement of D:
Sample Problem 2.1

## Slide 18: Static Indeterminacy
Structures for which internal forces and reactions cannot be determined from statics alone are said to be statically indeterminate.
Deformations due to actual loads and redundant reactions are determined separately and then added or superposed.
Redundant reactions are replaced with unknown loads which along with the other loads must produce compatible deformations.
A structure will be statically indeterminate whenever it is held by more supports than are required to maintain its equilibrium.

## Slide 19: Example 2.04
Determine the reactions at A and B for the steel bar and loading shown, assuming a close fit at both supports before the loads are applied.
Solve for the reaction at A due to applied loads and the reaction found at B.
Require that the displacements due to the loads and due to the redundant reaction be compatible, i.e., require that their sum be zero.
Solve for the displacement at B due to the redundant reaction at B.
SOLUTION:
Consider the reaction at B as redundant, release the bar from that support, and solve for the displacement at B due to the applied loads.

## Slide 20
SOLUTION:
Solve for the displacement at B due to the applied loads with the redundant constraint released,
Solve for the displacement at B due to the redundant constraint,
Example 2.04

## Slide 21
Require that the displacements due to the loads and due to the redundant reaction be compatible,
Example 2.04
Find the reaction at A due to the loads and the reaction at B

## Slide 22: Thermal Stresses
A temperature change results in a change in length or thermal strain. There is no stress associated with the thermal strain unless the elongation is restrained by the supports.
Treat the additional support as redundant and apply the principle of superposition.
The thermal deformation and the deformation from the redundant support must be compatible.